CORRIGENDUM No 2

Kotor, 22/01/2015

Corrigendum

CORRIGENDUM No 2 published on 22nd of January 2015: Technical specification for metal containers / ISPRAVKA Br 2 objavljena 22.01.2015: Tehnička specifikacija za metalne kontejnere

| Errata | Corrigenda |
| --- | --- |
| Municipal metal containers Volume at least 1.100 litters for communal waste Made of steel with double corrosion protection hot deep galvanization The thickness of the wall of the container at least 2mm with reinforcements Oval lid with rubber endings To provide at sides a system for hanging the unloading machine To provide at the bottom of the container an opening for discharging water 4-roll, swivel with brakes, load at least 200kg Containers shall comply with the standards and EN 840- 1,2,3 | Municipal metal containers Volume at least 1.100 litters for communal waste Made of steel with double corrosion protection hot deep galvanization The thickness of the wall of the container at least 2mm with reinforcements Oval lid with rubber endings To provide at sides a system for hanging the unloading machine To provide at the bottom of the container an opening for discharging water 4-roll, swivel with brakes, load at least 200kg Containers shall comply with the standards and EN 840-4,5,6 |